SPECIFICATION TEXT 
Secugrid® 20/20 Q1 

Pos.: ……. Quantity: …..…… Unit Price: ……………. Total Price: ………………… 
  
Geogrid, Secugrid® 20/20 Q1 or equivalent, made by NAUE GmbH & Co. KG, used as reinforcement under base and/or subbase courses over soft ground, supply and installation according to manufacturer’s installation guideline.

Secugrid® 20/20 Q1 is a geogrid made of stretched, monolithic, textured polypropylene flat bars (PP) with welded junctions, used for reinforcement in many fields of civil engineering, including landfill engineering, road construction and hydraulic engineering. The geogrid must not be coated with a separate polymer. Quantities are based on area to be covered. Wastage due to overlaps and cuts has to be included.

The following parameters have to be fulfilled:

Technical Data:

Raw Material:							Polypropylene (PP)

Nominal Tensile Strength:						≥ 20 / ≥ 20 kN/m
(md/cmd) (EN ISO 10319)

Tensile Strength at 2% Elongation:				8 / 8 KN/m
(md/cmd) (EN ISO 10319)

Elongation at Nominal Tensile Strength: 			≤ 7 / ≤ 7 %
(md/cmd) (EN ISO 10319)

Extensional Stiffness at 1% Strain:				400 / 400 kN/m
(md/cmd) (EN ISO 10319)

Radial Stiffness at 0.5% elongation:	 			≥ 334 kN/m
(EN ISO 10319)

Torsional Rigidity:							330 N-mm/deg
(GRI GG9)

Construction related strain:						0 %

Product Identification/Imprint:					max. 5.0 m distance

Roll Dimensions
Width x Length							4.75 m x 100 m

Following proof has to be provided:
•	Assessment of conformity according to DIN 18200
•	Quality Management System according to DIN EN ISO 9001
•	CE-Marking
•	Environmental-Product-Declaration (EPD)
•	Durability (Annex B, DoP) for at least 100 years in applications using natural soils with pH values between 4 and 9 and a soil temperature of < 25°C.

Proof of Delivery (POD)
Secugrid® 20/20 Q1
NAUE GmbH & Co. KG
Gewerbestraße 2
32339 Espelkamp-Fiestel
Tel.: +49 57 43 41 - 0
Fax: +49 57 43 41 - 240
E-Mail: info@naue.com
www.naue.com  
										Issue: 01.2021